## Slide 1
STA CCD Detector, Controller, and System Developments
Scientific Detector Workshop 2013
Florence, Italy
7-11 October 2013
Richard Bredthauer, Kasey Boggs, Greg Bredthauer
Semiconductor Technology Associates, Inc.
27122 Paseo Espada, Suite 1004
San Juan Capistrano, CA 92675
(949) 481-1595 | greg.bredthauer@sta-inc.net

## Slide 2: STA

## Slide 3: Introduction
Recent systems
Archon controller
High dynamic range dual output

## Slide 4: STA1600
Full 6” wafer imager
10560 x 10560 pixels
9 micron pixel
111,513,600 pixels per frame
16 outputs
Designed for US Naval Observatory

## Slide 5: STA4150 and STA3600
STA4150, 4k x 4k 15µm
VIRUS, 2k x 2k 15µm

## Slide 6: ARIES
STA4150 BI CCD – 4k x 4k 15 um, 4 Outputs
Archon Controller
Bonn Shutter
LN2 Cooling
Noise 2.7-2.9 e- 100 kHz
Full Well 249-265 ke-
Dark Current 0.8 e- / pixel / hour at -120C
HCTE > 0.9999997
VCTE > 0.99999998

## Slide 7: Vilnius University Observatory
STA3600 BI CCD – 2k x 2k 15 um, 4 Outputs
Archon Controller
Melles Griot UTS260 Shutter
Cryotiger Cooling
Noise 3.1-3.2 e- 100 kHz
Full Well 210-216 ke-
Dark Current 4.8 e- / pixel / hour at -100C
HCTE > 0.999999
VCTE > 0.999998

## Slide 8: NASA Ocean Radiometer for Carbon Assessment (ORCA)
STA4100 CCD – 512 x 128 TDI, 26 um pixels
Reflex Controller
8 Outputs at 20 MHz
Rotating telescope at 6 Hz, 33640 lines per revolution, 200 kHz line rate
2.5 uV / e-, 800 ke- full well

## Slide 9: Archon
12 slot modular controller, 20 kHz – 3 MHz
Copper or fiber gigabit ethernet TCP/IP interface
Up to 16 input channels, 16-bit 100 MHz ADCs, AC-coupled, 32-bit digital CDS
8 channel clock driver modules, 14-bit 100 MHz DACs, arbitrary waveform, programmable slew
6/24 channel DC bias modules, 16-bit DACs, voltage/current monitoring, programmable current limit

## Slide 10: High Dynamic Range

## Slide 11: Dual Outputs

## Slide 12
S1
S2
S3
S4
S1
S2
S3
S4
TX1
TX2
S4
Image Area
S1
S1

## Slide 13: CCD Output

## Slide 16: Performance
Low sensitivity alone: 104 dB 750000 DN full well, 4.5 DN noise
High sensitivity alone: 88 dB 250000 DN full well, 9.0 DN noise
Combined output: 114 dB 750000 DN full well, 1.5 DN noise equivalent

## Slide 17: Future Work