## Slide 1: Physics and applications of HgCdTe APDs
Ian Baker (SELEX) and Johan Rothman (CEA LETI)
09/10/2013

## Slide 2: Outline
Amplified photodetection
HgCdTe APDs physics and limitations
HgCdTe APD
HgCdTe APD applications with arrays (imagery) and single pixel detectors
Summary/perspectives

## Slide 3
Amplified photodetection

## Slide 4: Photodetection without internal gain
Photon signal
Readout noise sRO
Measured signal

## Slide 5: Photodetection with gain M
Internal photodetector gain M
M
The gain extracts the signal from the read-out nosie:
Low signals and/or high read-out noise :
0.001- 10 000 photons per observation time
M x Photon signal
Measured signal
RO noise

## Slide 6: Photodetector gain
Amplifies the signal to avoid SNR degradation due to the noise in the read-out electronics
Avoid loosing information … at best:
PD
gain
M
<M>
P(M)
sM
Excess noise
factor
Information conservation FM

## Slide 7
Increasing Gain
100mV
10mV
1mV
100µV
10µV
1µV
Signal (100 photons)
Photon noise (10 x√QE)
Electronic noise floor (FN)
Output voltage
Variance in gain multiplies photon noise x√F
(F=APD excess Noise Factor)
The object of avalanche gain is to increase the signal and photon noise above the fixed noise of the system
QEFR=QE/F should be maximal
Dark current noise should be minimal
Avalanche gain with low excess noise
MxSignal+ Read out noise (Noise floor)
Signal x QE
Low F
High F
~Photon
SNR
Amplified SNR
Dark current noise

## Slide 8
HgCdTe avalanche photodiodes
Typical gain curve
Gain Probability Distribution Function (PDF) and excess noise factor
Gain physics (geometry, lc, temperature)
Dark current limitations
Response time measurements

## Slide 9: HgCdTe Avalanche photodiodes (APDs)
Avalanche gain M>1000 to detect light from uv to the IR cut-off wavelength
Low excess noise factor F=1.1-1.3 (DRS, Selex, BAE, Raytheon, CEA)
Information conservation record : QEFR ~60-90 %
  QEFR < 0.5 for all other amplified detectors (PM, Si/II-V APDs, EMCCD..) !
Potentially the best detector for low photon detection and photon counting ?
Signature of multiplication without avalanche breakdown:
Single carrier multiplication: SCM !!!
Multiplication gain M
Reverse bias (V)

## Slide 10: Multiplication gain distribution estimated from single photon detection (CEA-LETI)
ADV=0 (flux zéro)
Dark events
Residual thermal flux detected with MWIR APD 4.6 µm)
Single photon events 1.6MHz (Ires=230 fA)
amp (V)
time (µs)
DCR=20-300 kHz
Seuil de <M> à 0.25 <M>
(DCR SWIR << 10 kHz)
Cold filter
APD hybridised on a
low noise ROIC
Noise/TC = 10-20 elect.
BW= 7 MHz

## Slide 11: Gain probability density function (PDF) of MWIR CEA-LETI HgCdTe APD at 80 K
Direct estimation of F= 1.25
The observed distribution enables high photon detection efficiency and the possibility to make photon number resolved (PNR) detection
  PDE=90 % at 0.5x<M>
  At the limit of PNR which is not possible with F>1.3 (F>=2 EMCCDs, SI/III-V APDs)
<M>=368
=1.25

## Slide 12: Linear mode photon counting with a CEA-LETI HgCdTe APD
Measured
Distributed dark-current generation
Measured 1 photon
APD gain PDF (+dark counts > 6 mV)
Distributed dark current generation
  Discrimination of non-amplified dark current events  Lower DCR
  Low noise on the amplified dark current  Noise on the dark current is the limiting parameter
DCR=20-300 kHz
Seuil de <M> à 0.25 <M>

## Slide 13
Heavy hole mass – 0.55m0 - low mobility
Holes must migrate to P-region to complete signal but otherwise do not take part in avalanche process hence low noise figure in HgCdTe
Foundations for MCT APD technology
Absorption of photons must be on the P-side to generate electrons for full benefit of avalanche gain.
Above a depletion width of 2.5-3.0µm1,2 alloy and phonon scattering starts to impact ionisation threshold voltage.
Below approximately 1.0 to 1.5µm there is risk of gain saturation and tunnelling currents.
1.5-2.5µm is technologically convenient
Avalanche gain in HgCdTe – illustration of single carrier (electron) history dependent impact ionisation
Recent literature
Johan Rothman, Laurent Mollard, Sylain Gout et al, “History-Dependent Impact Ionisation Theory Applied to HgCdTe e-APDs”, Jn of Elec Mat, Vol 40, No 8, 2011
Mike Kinch and Ian Baker, “HgCdTe Electron Avalanche Photodiodes”, Chapter 21, Mercury Cadmium Telluride - Growth, Properties and Applications, published by Wiley
hv
Potential energy
Low F due to spatially ordered multiplication
Electron and hole velocities limits the response time

## Slide 14: Influence of junction geometry on gain and noise Front side illuminated APDs with lc=4.6 µm at T=80 K
The gain is correlated with the average junction extension
  Increased threshold voltage, ~ constant slope
  Gain variation have been modeled as a function of xCd and T*
The excess noise has been found increases with increasing junction width
  Junction geometry fluctuations and enhanced uncertainty on the gain ?
Gain in CEA- APDs with different <wc>
<wC>
Planar N+n-P diodes in
EPL and MBE grown epitaxies
P~ 1016 cm-3
n-~1014 cm-3
N+
wc=0.8 µm
Tunnel currents
wc=1.4 µm
wc=2.4 µm
*Rothman et al, JEM 41, 2928 (2012)

## Slide 15: Gain as a function of lc at T=80 K CEA-Leti APDs
The gain decreases with decreasing lc
Exclusive electron multiplication with low F have been demonstrated down to lc= 2.2 µm (M=20 at 20 V)
  Limits the lowest possible dark current
The behavior of lower lc APDs is still not clear
  Onset of hole multiplication will strongly increase F and kill the particularity of HgCdTe APDs !

## Slide 16: Variation of the gain as a function of temperature (lc=3.3 µm at T= 80K)
293 K
220K
273 K
200K
180K
The gain decreases as a function of temperature
Local gain model  variation of the band gap and increased (low) energy dispersion *
*Rothman et al, JEM 41, 2928 (2012)

## Slide 17: Dark currents in HgCdTe APDs
1G. Perrais (Ph.D.S.), et al., J. electron. Mater., 36, 963 (2007)
2J. Rothman, et al., Proc. SPIE, 7834, 78340O 2010
Ieq_in (Mdark< M)
p
i
n
DC generation
Ieq_in decreases lc at constant gain and temperature
Dark current of 10 e/s have been observed for APDs with lc>3.0 µm  Low flux applications in astronomy
  Wavefront sensing, interferometry…
Ieq_in @ 80 K
Ieq_in (pA)

## Slide 18: 3 µm cut off FPA : dark measurement CEA-LETI/SFD FPA (RAPID)
Chart: T(K)
| 300 | 240 | 200 | 150 | 120 | 100 | 80
Jgr | 0.00010003 | 9.7841e-06 | 1.0261e-06 | 1.2817e-08 | 1.7761e-10 | 2.623e-12 | 5.0829e-15
Jdiff | 0.012762 | 0.000184 | 2.9853e-06 | 1.011e-09 | 4.2184e-13 | 2.0008e-16 | 2.4097e-21
FPA @ 3µm Jdark(6,3V) / M | 8.2522e-13 | 9.4634e-13 | 2.7925e-12 | 1.1851e-11 | 8.4458e-11 | 1.2737e-09 | 1.7293e-08 | 5.2942e-07
FPA @ 3µm Jdark (-0,2V) | 9.4508e-13 | 1.034e-12 | 1.1938e-12 | 2.0033e-12 | 6.223e-12 | 1.5581e-10 | 4.8239e-09 | 4.2887e-07
Under ~ 100 K, both currents reaches the same low level limited by the glow
At VAPD = -6,3 V, the GR dominates gain normalized current under 190 K
Would reach sub 5x10-15 A/cm² or 0.3 e-/s/pixel @ 80 K without glow
  At low bias, diffusion limited at temp. > 140 K
Notes: Here is plotted the evolution of the median current density with temperature for the 64 top lines of the FPA witch are less affected by the glow. Even for these lines we are limited by the glow at a value of about 50 elec per sec.
Anyway we can observe interesting things. First at high bias voltage, ...
At low bias …

## Slide 19: Response time variation as a function of bias and gain
Delayed response at high gain with constant exponential decay with t =270 ps
  Exponential decay due to impedance miss-matching
  Delayed response is due to a reduction of electron and holes velocities ve=3.5x106 cm/s, vh=1.5x106 cm/s
    BW  10 GHz in narrow junctions (optimized resolution~20 ps)
    Close to Independent on temperature
Localized injection (APD center)
T= 80 K
-- M= 1.( (6 V), risetime 50 ps
-- M=5 (10 V)
-- M= 35 (14 V)
-- M= 70 (16 V)
-- M= 130 (18 V), risetime 100 ps

## Slide 20: High gain perspectives
Gain in excess of 1000 enables photon-counting with sub ns resolution using deported transimpedance amplifier (TIA)
  But at reduced BW is expected due to the large xj ~ 2 GHz
xj=3.4 µm APD at T=180 K
Stable gain M=1800 at 28 V
Impulse response with substrate
(edge and center response)
At 28 V and M= 1800 (180 K)

## Slide 21: Electronic engineers view of an avalanche photodiode in HgCdTe
The very impossible amplifier
Voltage controlled gain at the point of absorption
Little additional noise
Up to (10) GHz bandwidth
Requires no Si/Ge/III-V real estate
Negligible power consumption
Negligible non-uniformity
Shrinkable to the micron scale
Fundamentally highly stable
Ian Baker : Quite a useful component!

## Slide 22
HgCdTe APD technologies
SELEX, DRS, Raytheon, BAE, LETI

## Slide 23: Avalanche photodiode technologies:
Avalanche region n-
Graded composition
P+ to p-
N+
hv
P absorber
Avalanche region n-
N+
hv
LPE/via-hole technology
Excellent breakdown quality
High avalanche gain
Panchromatic spectral response
MOVPE/mesa technology
Higher operating temperature
High avalanche QE
Few pixel defects
Low excess noise F
Wafer scale processing
Selex (UK) and DRS (US)
Selex (UK)

## Slide 24: Avalanche photodiode technologies :
Avalanche region
Absorbing layer
Collection layer
hv
hv
Planar LPE technology
Excellent breakdown quality
High avalanche gain
Panchromatic spectral response
Fast response
Low gain dispersion
Low dark current
High operability
MBE/mesa technology
Higher operating temperature
High avalanche QE
Fast response
Low F
CEA-Leti/Sofradir (Fr) and BAE (US)
Raytheon (US) ? (cf. Don Hall)

## Slide 25
HgCdTe APD applications
MWIR HgCdTe APDs for imagery
SWIR HgCdTe APDs for imagery
Singel element applications

## Slide 26: Typical performance of MWIR HgCdTe APDs at 80 K
Multifunctional thermal and/or active imaging
  Detection and identification
  Aerospatiale navigation
  Bio-medical research/cancer detection
FPAs for short integration times (30 ns – 1 µs) have been developed by Selex, DRS, CEA/SFD and Raytheon
Linear APD gain record
M=12 000 (SFD 2011)
12 000

## Slide 27: SWIR HgCdTe APDs
Reduced gain at constant reverse bias
Reduced dark current at constant bias and temperature
Passive low flux fast frame rate imaging
  SELEX SAPHIRE Presentation by Gert Finger
  RAPID CAMERA (LETI/SFD/IPAG/ONERA/LAM), Presentation by Philippe Feautrier
High operating temperature (200-300 K) for high BW applications :
  active imaging (2D, 3D)
  single element detection …
80K performance
0.4-10 ns
(< 0.05aA) ?

## Slide 28: Uniformity of avalanche gain in LPE/via hole technology at SELEX
Avalanche gain adds virtually nothing to non-uniformity
Depends only on voltage and alloy composition

## Slide 29: Example of avalanche gain in astronomy using LPE/via hole technology SELEX Saphira
APD sensor
Cutoff - 2.45 µm
Temperature - 40K
Int. time – 5.06ms
Bandwidth – 5MHz
APD gain – 33x
Courtesy: Gert Finger - ESO
In photon starved applications can get two orders of magnitude improvement in sensitivity compared with conventional sensors

## Slide 30: MOVPE technology for advanced eAPDs at SELEX
Mesa isolation provides photon confinement for high absorption efficiency and reduction of crosstalk and stray light export
Narrow bandgap N-type for avalanching
All photo-electrons experience avalanche gain
Bandgap engineering to minimize breakdown, dark currents and response time

## Slide 31: Ultra fast SWIR e-APD FPA and Camera
Minalogic (Rhone-Alpes/Isère) funded project :
  Partners:
    FPA developement : CEA-Leti, Sofradir
    Camera development and demonstration : IPAG, Onera, LAM…
Measured Detector performance
  320 x 240 pixels 30 µm pitch APD array : LETI on top
  8 outputs of 60 row @ 20 MHz : Sofradir bellow
  Wavelength: 0.2 – 3.2 µm
  M=10-30, QE/F~0.7
  Full frame readout: 1500 Hz (0.67 ms) min, up to 2 kHz, pixel frequency 20 MHz
  Windows: one rectangular window of any number of lines, each line read in 2.7 µs
    Maximum “fram rate” = 370 kHz
  System Noise: ~ 2-3 photons at 1500 Hz frame rate (with gain x15)
  Median Dark current : ~ 10 e/s/pixel
  Full well: 40 000 e (with gain x1)  low SNR images
  Gain and dark noise operability : >99.5% at low flux
31
26/09/2011
Ultra fast and sensitive

## Slide 32: 3.3 µm lc RAPID FPA : VAPD = -8 V
FPA photonic measurement @ TFPA = 80 K, VAPD = -8V
Gain
<M> = 31 ; Median = 30,8
99,8 % Operability (+/- 50%)
  Excess noise
  <Fmeas> = 0,99
  Hyp. : quantum efficiency increase with bias hM>h1
Notes: Now we will go on with the 3.3 µm cut off test results.
For a reverse bias voltage of 8 volts we get a gain of 31 with a very good operability.
We have also evaluated the excess noise factor. We get a mean value under 1 witch is not realistic. We think that it comes from an evolution of the effective quatum efficiency with the diode bias. In that case, the measure gives the true value of F multiply by the ratio between the low bias quantum efficiency to the high bias one.

## Slide 33: 3,3 µm lc RAPID FPA: QEFR
QEFR is the only measurable FOM
It can be estimated from measurable FOM
<QEFR> = 0,57 for at a gain 31 !
Notes: So as we can’t access to the true value of F, the good figure of merit to quantify the information conservation is the quantum efficiency excess noise ratio. By definition this is the quantum efficiency at high bias voltage divide by the true value of F. As we have seen before this true F value is not accessible from direct measurement. Fortunately it can be measurable parameters, the unity gain quantum efficiency and the previously measured F factor. In our case we get a mean array value of 0.57.

## Slide 34: 3,3 µm lc RAPID FPA : dark noise
FPA input referred dark noise @ M=31 : end user FOM
  TFPA = 82 K, VAPD = -8 V, Tint = 600 µs
  Pixel by pixel input referred dark noise evaluation
  Mean noise = 1,7 e- ; Median 1,5 e-
  99,54 % of pixels with noise < 10e-
Notes: For this same FPA, the input referred noise in the dark at 600 µs integration time reaches a mean value of 1,7 electrons. Taking into account the previously calculated QEFR this gives a equivalent photon noise lower than 3 photons per pixel per frame.

## Slide 35: Single element (mini-arrays )
System requirements and/or Optimisation is different than in FPA applications:
    BW/operating temperature/sensivity/active area…
Spectroscopy
-nanoscience/biochemistry
TC=1s-1ns
Signal=0.001-10000 photons
Direct detection /Lidar/optical meas.
-Gaz analysis /TOF/
TC=50 ns- 10ps
Signal 0.001-100 photons/TC
Photon counting (number resolved)
-Quantum physics/
/high-energy phys./astrophys./biomed.
TC=1s-10ps
Telecom
TC=10 ns-10ps
Signal 1-1000 photons

## Slide 36: Detection system adapted to system requirements
)
Deported amplifier
Hybridized amplifier
APD
APD
High operating temperature
  BW 1Hz à 60 GHz
  Noise 300-1000 électrons/TC
  Compatible low T TEC <180 K
LIDAR, Télécom, Bio-médicale, science (magnéto-optique)
High sensitivity
  BW max ~ GHz
  noise 10-100 électrons/TC/pixel
    Low temperature
  Intelligent MUX
  Photon counting resolution
Optique quantique/ LIDAR/fluorescence moléculaire/spectroscopie…
Cold finger
(TEC cooled)
Cold finger

## Slide 37: HgCdTE APD for LIDAR application with deported TIA
System optimization/ Operating temperature (high/low) :
Signal ↔BW ↔ TIA noise ↔ Surface ↔ gain ↔ lc(xCd)
2 Demonstrators with deported TIA are currently being assembled at CEA
  BWTIA=30 MHz, iTIA<1 pA/Hz0.5 , Top=160-200 K (TEC), f>100 µm : CO2, H20, CH4 LIDAR
  BWTIA=480 MHz, iTIA=2.1 pA/Hz0.5 Top=180-220 K (TEC): TOF, free space telecom
Expected performance, iTIA= 1pA/Hz0.5 f=120 µm ,lc=3.15 µm à 180 K
NEPh
Gain
Limited by TIA noise (gain(T, xCd)
Limited by dark current (Top, f, xCd)

## Slide 38: Performance MEATS-1 detector(CEA)
BW TIA=450 MHz
BW APD=50 MHz (diffusion limited)
NEP= 20 fW/Hz0.5
Active area 160 µm
Top=192 K
Impluse response of 30 µm diode at 1 nW input power (APD gain=50)

## Slide 39: MEATS-1 for lunar laser communication with ESA and NASA
RF MEATS detector is waiting for photons from the moon on Tenerife

## Slide 40: Photon counting detector perspectives
APD- with low noise ROIC and/or fast amplifier
  Quantum physics and telecomunications, Lidar, spectroscopy, fluorescence life time, real-time physics
Optimal detector performances (applications)
  High PDE : ok > 90 %xQE
  Low DCR : ~ok (< 1 kHz in SWIR) at low temperature
  Photon number resolution : ok
  Temporal resolution 20 ps-10 ns
  Max repetition rate : 1- 10 GHz: possible, with external TIA and high gain > 300
  Spatial resolution -> photon counting imager : possible
First CEA/Leti
photon counting
demonstration,
BW=7 MHz

## Slide 41: Summary
HgCdTe APDs detects 0 to 1000 photons with minimal loss of information from uv to IR
  High gain M>1000
  Record high QEFR~60-80 %
  Idark (Ieq_in) down to electrons/s
HgCdTe APD FPAs for active and passive imaging have been demonstrated with performances close to non-amplifed FPAs
  Low noise, high uniformity, high operability > 99.5 %
Single/multi element detectors
  Large horizon of applications
  2 demonstrators are under developments
    BW=30 et 500 MHz, NEPh< 10 photons (NEP< 10 fW/Hz0.5) à Top~200K
  Demonstration of photon counting
Perspectives
  Cameras and detectors with optimized QE, F, Ieq_in, BW, operating temperature
  Photon counting arrays and detectors with photon number resolution
  Single photon detection with sub-20 ps resolution at record high PDE

## Slide 42: Merci de votre attention

## Slide 43
Increasing gain (bias voltage)
100mV
10mV
1mV
100µV
10µV
1µV
Signal (100 photo-electron)
Photon noise (10e rms)
Electronic noise floor (FN)
Output voltage
F – Noise Figure Q – Quantum efficiency FN – Fixed noise T – Transfer function M – Avalanche gain
APD system sensitivity:
Noise Equivalent Photons
NEPh (SELEX def)
Need a new figure of merit for APDs
as noise is now a combination of photon noise, gain noise and system noise
Avalanche gain in astronomy applications

## Slide 44: Example of NEPh-Selex in a practical system
x3
x6
x12
x25
x50
Cutoff – 4.4µm
Fno - 4.5
Quantum efficiency – 0.7
Temperature – 90K
Fixed noise - 50µV rms
Noise Figure – 1.3
Actual NEPh effected by stray light and dark current
NEPh drops pro rata with avalanche gain until the photon noise becomes significant.
It then limits to some value dependent on the stray light and dark current.
The ultimate sensitivity is noise figure/QE (1/QEFR)
Ultimate NEPh is noise figure/QE=1/QEFR

## Slide 45: Dark measurement on a RAPID retina with 3 µm cut off
Evaluate the dark current (low bias) and gain normalized dark current (high bias) evolution with FPA temperature
  At low temp. Long Tint is needed (up to 4s)
Example of short and long Tint images @ 80 K
VAPD = -0,2 V, Tint = 2 s
VAPD = -0,2 V, Tint = 600 µs
  ROIC glow is observed for long Tint, doesn't affect short integration time EO performances
Notes: Now I will switch on measurement in dark conditions. The FPA was use to evaluate the dark and gain normalized dark current evolution with photodiodes temperature. To get a significant signal level we had to use long integration time. As an example, you can seen here the raw images that we get for 600 µs integration time and 2s. We have observed an excess of current coming from the bottom of the FPA. We know now that this due to ROIC glow.
As we will see later this glow doesn’t affect the FPA performance at the short integration times needed for astronomical applications.

## Slide 46: Response time modelling using the charge drift and multiplication model*
Electron and hole velocity is estimated from the adjustment of the rise time (M given by gain measurements)
RC constant is close to constant for each sample
  RC1A=270 ps  BW=600 MHz
  Probably due to parasitic impedance in the interconnection circuit
Short-circuit response
M=60, ve =3.5x106 cm/s, vh=1.9x106 cm/s
FWHMlaser=52 ps
RC=270 ps
Sample 1A (xj=2.2 µm)
18V bias, M=60
*Perrais et al, JEM 38, 1790 (2009)

## Slide 47: Physics of the gain Local gain model
wc | aEg/q | b
(µm) | (V/cm)1-c | (V/cm)
0.77 | 22.2 | 3.24E+04
1.40 | 22.4 | 3.28E+04
2.40 | 22.6 | 3.25E+04
Excellent fit of gain on-set and gain saturation
  a and b independent of junction width wc
a: saturating high field multiplication efficiency
b: critical field at which the electrons the electrons start to multiply
c=0.6
lc=4.6 µm (80 K)

## Slide 48: Electron and hole velocities in a xj=2.2 µm APD
The low field low gain electron velocity decreases
The high field high gain electron and hole velocities are close to independent of the temperature
  ve~3.5x106 cm/s and vh~1.5-2 x106 cm/s at M~100
  But it reduces at high temperature at constant gain (as the same gain requires higher bias at higher temperature)
Electron junction drift velocity ve
Hole junction drift velocity vh

## Slide 49: High BW perspectives at gains of 100 and T= 200-300 K
xj=0.8 µm, ve=3.5x106, vh=1.9x106 short-circuit limit 
FWHM< 50 ps, BW = 9 GHz !