## Slide 1: Optical AO WFS Detector Developments at ESO
Mark Downing, Johann Kolb, Norbert Hubin, Javier Reyes, Manfred Meyer European Southern Observatory ESO (http://www.eso.org) Martin Fryer, Paul Jorden, Andrew Payne, Andrew Pike, Rob Simpson, Paul Jerram, Jerome Pratlong e2v technologies ltd (http://www.e2v.com)
Bart Dierickx, Arnaud Defernez, Benoit Dupont
Caeleste, Antwerp, Belgium (http://www.caeleste.be)
Jorge Romero
University of Málaga (http://www.uma.es) Philippe Feautrier, Eric Stadler Institut de Planétologie et d’Astrophysique de Grenoble (http:// http://ipag.osug.fr/) Jean-Luc Gach, Philippe Balard, Christian Guillaume
Laboratoire d'Astrophysique de Marseille LAM (http://www.lam.oamp.fr)

## Slide 2: Outline
L3Vision CCD220 – developed by e2v on behalf of ESO/OPTICON
  Deployment of AONGC Cameras on VLT AO instruments
  Test Result Summary
    Trades made with Deep Depletion CCD220
    Improvements of the HV Clock Design
    SCTE
Next challenge → LGSD/NGSD
  Large CMOS Visible AO WFS Imager for the ELT to sample the spot elongation of Laser Guide Stars
  Specifications
  Wavefront Sensor Architecture and Design
  First results

## Slide 3: e2v L3Vision CCD220
Store
Area
Image Area
240x120
24□µm
Store
Area
Image Area
240x120
24□µm
OP 1
OP 2
Gain
Registers
OP 3
OP 4
Gain
Registers
OP 8
Gain
Registers
OP 7
OP 6
Gain
Registers
OP 5
e2v CCD220:
    240x240 24 µm pixels
    Split frame transfer CCD
    8 L3Vision EMCCD outputs
    < 0.1 e- RoN at 1,500 fps
    Integral Peltier for cooling to -50ºC
Metal Buttressed
2Φ 10 Mhz Clocks
for fast image to store transfer rates.
Store slanted
to allow room for multiple outputs.
8 L3Vision Gain Registers/Outputs
Each 15Mpix./s.

## Slide 4: Deployment of AONGC WFS Cameras
HAWKI
SPHERE
ERIS
MUSE

## Slide 5: CCD220 Impressive (Measured) Test Results
Requirement | Measured | Specification
Frame Rate: | > 1,500 fps | >1,200 fps
Read noise at gain of 300 | < 0.2 e- | < 1.0 e-
Image Area Full Well: | > 160 ke- | > 5,000 e-
Cosmetics: # of traps, bright/dark defects | 0 | < 25
Dark Current: 1200fps & -40ºC 100fps & -50ºC | < 0.02 e-/pix/frame < 0.05 e-/pix/frame | < 0.04 e-/pix/frame
Key goal specs are met
Deep Depletion (highly sought after for better red response) is working as good as the standard silicon devices.
Next Steps:
Increase frame rate to 2,500 fps to extend use to E-ELT XAO (Extreme AO).
Test shuttered device CCD219 for pulsed laser guide star applications.

## Slide 6: Trades made with Deep Depletion Device
Deep Depletion enabled devices to be built out of thicker silicon (40µm) for better red response;
  Highly sought after for applications using Natural Guide Stars.
  75% improvement

## Slide 7: Trades made with Deep Depletion Device
Deep Depletion enabled devices to be built out of thicker silicon (40µm) for better red response;
  Highly sought after for applications using Natural Guide Stars.
During charge integration if the image area is simply run into inversion for lowest dark current like the Std Si device then obtain very poor PSF.
  Has an additional “p” well implant for EMCCD to work.
  A minimum bias is required to “punch-through” (depletion to extend beyond) this “p” well.
Std Si
Deep Depletion

## Slide 8: Trades made with Deep Depletion Device
Very High Level
Deep Depletion enabled devices to be built out of thicker silicon (40µm) for better red response;
  Highly sought after for applications using Natural Guide Stars.
During charge integration if the image area is simply run into inversion for lowest dark current like the Std Si device then obtain very poor PSF.
Solution is to use Tri-Level clocking to obtain the best trade between PSF and Dark Current.
  Low Level that takes the device into inversion for low dark current.
  High Level just right for good frame transfer and low Clock Induced Charge.
  Very High Level for integrating charge to tune the PSF.
Frame Transfer
Integration
-8V
-0.5V
Image Area Clock
Low Level
High Level

## Slide 9: Adjust Very High Level to Tune PSF
Min.
Goal
Chart: PSF Vs Integration Voltage
| -8 | -6 | -4 | -2 | 0 | 2 | 4 | 8 | 12 | 16
X IPh=-6V | 7.24 | 5.32 | 2.82 | 1.97 | 1.1622 | 0.81837 | 0.56837 | 0.41735 | 0.37347 | 0.3602
VInteg=-8V
VInteg=-4V
VInteg=0V
VInteg=4V
VInteg=8V
VInteg=12V
Min.
Goal
Min met at > 2V.
Goal met at > 8V.

## Slide 10: and trade with CIC and Dark Current
As expected CIC does not increase with integration voltage.
Once out of inversion, dark current does not increase further with integration voltage.
  thanks to “Intrinsic dithering” – uses the fact that after inversion holes that have migrated into Si/SiO2 I/F have long release time constant.
Goal Dark Current and PSF specs are met at 8V.
1200fps
100fps

## Slide 11: Improvement to Design of HV Clock
Design → LC resonant circuit
  switch, transformer, and capacitor (includes that of the CCD phases);
  tune to resonate at pixel (switch) frequency;
  simple, low power dissipation.
First implementation:
  levels stabilized by simply correction for the integrated difference between peak and reference level.
  Problem is that it does not respond quickly to transients/disturbances.
Both measurements and simulations prove that the resonance circuit is very sensitive to any changes in the load. The load (the CCD) changes during read out due to changes in clock (inter) capacitances.
Peak Detector
Peak Detector
ON
OFF
~ 0V
20-50V
Tpixel

## Slide 12: At Unity Gain: Flat field is very flat

## Slide 13: However at gain, flat field varies with readout
  Oscilloscope shows the amplitude of the HV Clock varies during a frame read out and variation is proportional to illumination level.

## Slide 14: Solution is to use full PID controller in the feedback loop
A properly designed PID controller should respond quickest to disturbances.
Peak Detector
Peak Detector
PID
PID

## Slide 15: Original design with step input

## Slide 16: Optimised design with step input

## Slide 17: “Proof of the Pudding”
Afterwards
Before

## Slide 18: SCTE - Long Tail of Residual Charge
520 gain elements
Outputs
60 register elements
Store section
By reverse clocking the serial register able to get all charge in a single pixel

## Slide 19: SCTE - Long Tail of Residual Charge
SCTE gets worse with higher gain and signal thus need to operate at lowest gain for the application.
To keep gain low, need to optimize for low read out noise at unity gain.
Lower range expanded
Gain x 400
VROL=-5V
L3Vision has long tail of residual charge

## Slide 20: The need for good SCTE
With Shack Hartmann WFS, if SCTE does not vary much with signal then it is simply an offset in the centroid that can be subtracted.
Sub-aperture
However, with pyramid WFS, SCTE appears as cross-talk into neighboring sub-apertures → spec. is < 1%.

## Slide 21: Gain 400; SCTE Vs Serial Clock Low Level
SCTE < 1% is only met when VROL = -7V; i.e. when serial register is clocked into inversion.
Fortunately, Clock Induced Charge does not increase significantly.
Tells us something about where the charge is being trapped – Si-SiO2 I/F
Strategy Followed:
Set up output amplifier biasing and serial register to maximize CIC and dark current as this guarantees that all charge is being detected.
Amp 0
Amp 5
VROL=-4V
VROL=-5V
VROL=-6V
VROL=-7V
Best Amp
Least Best Amp

## Slide 22: Gain 400: SCTE < 1% for all amplifiers with VROL=-7V
Amp 0
Amp 4
Amp 1
Amp 5
Amp 2
Amp 6
Amp 3
Amp 7

## Slide 23: Outline
L3Vision CCD220 – developed by e2v on behalf of ESO/OPTICON
  Deployment of AONGC Cameras on VLT AO instruments
  Test Result Summary
    Trades made with Deep Depletion CCD220
    Improvements of the HV Clock Design
    SCTE
Next challenge → LGSD/NGSD
  Large CMOS Visible AO WFS for the ELT to sample the spot elongation of Laser Guide Stars
  Specifications
  Wavefront Sensor Architecture and Design
  First results

## Slide 24: Block Diagram of Full Size Device; LGSD
Highly integrated
  All analog processing on-chip:
    correlated double sampling (CDS),
    programmable gain of x1/2/4/8 on the fly,
    9/10 bit single slope ADCs,
    total effective 12 bit data conversion
  20 top + 20 bottom rows processed in parallel to slow the read out per pixel (34µs) and beat down the noise.
  Fast LVDS serial interface to outside world
    simple digital interface;
    power consumption similar to high speed drivers to transport analog signals off-chip;
    better guarantee of achieving and maintaining low noise performance.
84x84 Sub-apertures
each 20x20 pixels
Pre-Amp & Gain of x1/2/4/8
20x1760 single slope ADCs
Multiplexer/serializer
Y-addressing
Control
Logic
Y-addressing
Control
Logic
Pre-amp & Gain of x1/2/4/8
20 x1760 single slope ADCs
44 LVDS Serial Links
44 LVDS Serial Links
Multiplexer/serializer
Control
Logic
Control
Logic
1760x1680
pixels
Natural Guide Star Detector (NGSD)
  pioneering scaled down demonstrator
  ~ ¼ of full size → non-stitched

## Slide 25: Specifications of the LGSD (NGSD) Physical characteristics
Pixel array (Refn pixels - 40 columns) | 1760x1680 (880x840 pixels in NGSD) - 5x6cm requiring stitched design (>> max. reticle 25.5x32.5mm)
Technology | Thinned backside illuminated CMOS 0.18µm – TowerJazz APD3; 6 metal layers
Silicon | High resistivity 1000 ohm-cm → targeting thickness of 12µm
Pixel pitch | 24µm
Pixel topology | 4T pinned photodiode pixel with low noise threshold transistors; slit wafer run more speculative ultra low threshold → 1e- goal
Array architecture | 84x84 time coherent “sub arrays” of 20x20 (8x8 NGSD) pixels - LGSD image area size of 4x4cm
Shutter | Rolling shutter in chunks of 20 rows → synchronous temporal detection within a sub-aperture.

## Slide 26: Specifications of the LGSD (NGSD) Read out
Number of rows read in parallel | 40 (20 in NGSD) rows in parallel
Number of ADC’s | 40x1760 (20x880 in NGSD) at 9/10 bits
Number of parallel LVDS channels | 88 (22 in NGSD)
Serial LVDS channel bit rate | 210 Mb/s baseline, up to 420 Mb/s (desired)
Frame rate | 700 fps up to 1000 fps with degraded performance 2 to 3 Gpixel/s = 20 to 30 Gb/s over 88 parallel LVDS channels
Power dissipation | < 5W , (NGSD 0.5W) including the 88 LVDS drivers
Actual LVDS driver dissipation per channel | 6.0mW at maximum data rate; 4.5 mW in sub-LVDS

## Slide 27: Specifications of the LGSD/NGSD Performance
Pixel full well QFW | > 4000 e-
Linearity to full well | < 5%
Read noise including ADC | < 3.0 e-RMS
Image lag | < 2 %
Dark Current | < 0.5 e-/pixel/frame
QE | > 90% at 589nm; optimized for the red → BackSide Illumination (BSI)
Point Spread Function | < 0.8 pixel FWHM
Cosmetics | < 0.1% bad pixels
Already verified in Technology Demonstrator

## Slide 28: Video Chain – single slope ADC
comparator output
Gray code
ramp
offset
0
512
Latch code
video
reset
signal
transfer
reset
Single slope ADC chosen for robustness, excellent low noise and linearity (DNL).
Good compromise between speed, precision, power consumption, and area occupied
Column
bus
1
VRST
VSF
reset
p-Si
2
transfer
4
n+
p+
3
select
4T pixel
Ramp
x1
x2
x4
x8
-
+
Pre-Amp
Comparator
Gray Code
9/10
D
Q
Clk
-
+
A
Copy
LVDS Out
110MHz DDR
Sync
Parallel to Serial
D
Q
Clk
Double Register
B
SN
PPD

## Slide 29: LGSD Tentative Stitching Plan
22x42
sub- apertures
5.28mm
Yaddressing
Yaddressing
10.56mm
11 LVDS
&
8800 column ADCs
Corner
Corner
Corner
Corner
8800 column ADCs
&
11 LVDS
20.16mm
10.08mm
Reticle View
Corner
Yaddressing
22x42
sub- apertures
11 LVDS
&
8800 column ADCs
22x42
sub- apertures
11 LVDS &
8800 column ADCs
22x42
sub- apertures
11 LVDS &
8800 column ADCs
22x42
sub- apertures
Corner
Yaddressing
Yaddressing
Yaddressing
Corner
8800 column ADCs
&
11 LVDS
8800 column ADCs
&
11 LVDS
8800 column ADCs
&
11 LVDS
8800 column ADCs
&
11 LVDS
Corner
10.56mm
10.56mm
10.56mm
10.56mm
11 LVDS &
8800 column ADCs
20.16mm
20.16mm
22x42
sub- apertures
22x42
sub- apertures
22x42
sub- apertures
22x42
sub- apertures

## Slide 30: NGSD anticipates scaling to LGSD
5.28mm
Yaddressing
Yaddressing
22x42
sub-apertures
10.56mm
11 LVDS
&
8800 column ADCs
Corner
Corner
Corner
Corner
8800 column ADCs
&
11 LVDS
20.16mm
10.08mm
Reticle View
Corner
Yaddressing
22x42
sub-apertures
11 LVDS
&
8800 column ADCs
11 LVDS &
8800 column ADCs
11 LVDS &
8800 column ADCs
Corner
Yaddressing
Yaddressing
22x42
sub-apertures
22x42
sub-apertures
Yaddressing
Corner
8800 column ADCs
&
11 LVDS
8800 column ADCs
&
11 LVDS
8800 column ADCs
&
11 LVDS
8800 column ADCs
&
11 LVDS
Corner
10.56mm
10.56mm
10.56mm
10.56mm
11 LVDS &
8800 column ADCs
20.16mm
20.16mm
22x42
sub-apertures
22x42
sub-apertures
22x42
sub-apertures
22x42
sub-apertures
22x42
sub-apertures

## Slide 31: Read out
88x42 Sub-Apertures
South Half-Array
Center line
88x42 Sub-Apertures
North Half-Array
reset, select & transfer
20 sets of row select lines per SA
20x20 pixels per SA
4T 24um pixel
20 lines per column of pixel
Sub- aperture row addresses
(1 of 42)
Random address Control
Sub- aperture row addresses
(1 of 42)
Random address Control
Timing, clocks and biases
ADC Gray Code BUS
ADC Ramp
20 rows of column bias & pre-amp with gain of x1/2/4/8 settable SA by SA
20 rows of comparators (35,200)
20 rows of Registers A
LRC40 Checksum Calculator
Parallel to serial
LVDS Outputs
110MHz Clock DDR
Sync
Copy
Gain
20 rows of Registers B
D
Q
D
Q

## Slide 32: Summary
CCD220:
Both Std Si and Deep Depletion variants of the CCD220 are working extremely well, production run of cameras is nearing completion, and our instrument project managers are now very happy.
LGSD/NGSD:
ESO has formed a good partnership with e2v and Caeleste.
The design of the NGSD is complete and in fabrication.
Extensive simulations have confirmed correct operation and performance.
Devices will be available in the coming months for testing

## Slide 33: Thank You
This work has been "partially funded by the OPTICON-JRA2 project of the European Commission FP6 and FP7 program, under Grant Agreement number 226604"

## Slide 34: TVP – optimises pixel deisgn
Optimize the pixel design to find best trade between image lag, linearity, gain, and noise (white and 1/f) by testing:
pixel variants with different transfer gate and transistor geometries;
different threshold voltages of the nmos transistors;
extra implants to improve image lag.
1
VRST
Column
bus
VSF
reset
p-Si
2
3
transfer
4
n+
p+
select
transfer gate
reset
select
Pinned photodiode
p implant
p+ implant